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ZIB0 ZHONGNAN PHARNACEUTICAL PACKAGING MATERIALS C0.,LTD QIGUO SFEIZER

QIGUO PLASTICS





A7,Jinyingu Pioneer Park,Zhantai Road,Linzi Economic Development Zone,Linzi District,Zibo City,Shandong Province,China

TEL:+86-533-7507100 FAX:+86-533-7508201 
CERTIFICATE OF ANALYSIS

  Date of Test: Jul. 28,2020     Date of Report: Aug. 3rd,2020       Invoice No.:VNT20070906
	  Product
	Amber PVC/PE
	Size
	PVC 0.28mm/PE 0.05mm×345mm

	Batch No.
	VNT20070906
	Standard
	YBB00232005-2015

	QTY
	18025.8kg
	Maker
	 PVC/PE PLANT

	MFG DATE
	Jul. 20th,2020    
	EXPIRY DATE
	Jul. 20th,2023

	Item
	Specification
	Test Result
	Conclusion

	Appearance
	Sheet should be free from color difference,wrinkledness,dirt,foreign particles,perforation,fisheye’s diameter＞1.3mm：never discovered,≤1.3mm：no more 3/100cm2
	YES
	Qualified

	Width
	345±1mm
	345
	Qualified

	Thickness
	0.33±0.01mm
	0.32-0.34
	Qualified

	Water Vapor Transmission
	≤2.5g/(m2·24h)
	1.3
	Qualified

	Oxygen Transmission
	≤20cm3/(m2·24h·0.1MPa)
	9
	Qualified

	Heating Shrinking rate
	≤±6.0%
	-2，+1
	Qualified

	Heating Sealing Strength
	≥6N/15mm
	14
	Qualified

	Tensile strength
	MD:≥40.0MPa
	55
	Qualified

	
	TD: ≥40.0MPa
	55
	Qualified

	Falling Ball Impact Brittle Rate
	No more than two pieces of damage in TD.
	YES
	Qualified

	
	No more than two pieces of damage in MD.
	YES
	Qualified

	Remainder of solvent
	≤10mg/m2
	Not be detected.
	Qualified 

	Test of Extraction
	Degree of  Amber
	Ought to be Amber
	Amber
	Qualified

	
	Test of Oxidation
	Difference of Titer ≤1.5 ml
	0.7
	Qualified

	
	Heavy Metal
	≤0.0001%
	＜0.0001%
	Qualified

	
	Non-

volatile
	Water
	≤30mg/100ml
	3
	Qualified

	
	
	65%Ethanol
	≤30mg/100ml
	4
	Qualified

	
	
	n-Hexane
	≤30mg/100ml
	5
	Qualified

	Vinyl Chloride Monomer
	≤1PPM
	<1
	Qualified

	Micro-

organism
	Total aerobic bacteria
	≤1000cfu/100cm2
	14
	Qualified

	
	Mildew & microzyme
	≤100cfu/100cm2
	<10
	Qualified

	
	Coliform
	Non-permit
	Not be detected.
	Qualified

	Conclusion
	This production is qualified.


Approval：                        Check:              Test:                       
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